LAKES OIL N.L. CUTTINGS DESCRIPTIONS WELL NAME: BOUNDARY CREEK No.2 DATE: 26-10-2005 GEOLOGIST: David Horner PAGE: 1

| Interval (m) | % | Description |
| --- | --- | --- |
| 1176-1179 | 100 | SANDSTONE: light to medium green grey, very fine to medium, dominantly fine to medium, subangular to subrounded, moderately sorted, moderate silica and strong calcareous cements, abundant white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly detritus, trace calcite and a brick red mineral vein infill, hard, very poor visual porosity, no oil fluorescence. |
| 1179-1182 | 90 | SANDSTONE: light to medium green grey, very fine to medium, dominantly fine to medium, subangular to subrounded, moderately sorted, moderate silica and strong calcareous cements, abundant white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly detritus, hard, very poor visual porosity, no oil fluorescence. |
|  | 10 | CLAYSTONE: off white to medium grey to medium green grey to medium brown grey, very silty - grades to siltstone, often very finely arenaceous with altered lithic grains, trace black carbonaceous flecks, common black coal detritus, trace micromica, moderately hard, subfissile. |
| 1182-1185 | 30 | SANDSTONE: light to medium green grey, very fine to fine, dominantly very fine, subangular to subrounded, moderately sorted, moderate silica and calcareous cements, abundant white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly detritus, hard, no visual porosity, no oil fluorescence. |
|  | 70 | CLAYSTONE: off white to medium grey to medium green grey to medium brown grey, very silty, often very finely arenaceous with altered lithic grains, trace black carbonaceous flecks, common black coal detritus, trace micromica, moderately hard, subfissile. |
| 1185-1188 | 90 | SANDSTONE: light to medium green grey, very fine to fine, dominantly fine, subangular to subrounded, moderately sorted, moderate silica and calcareous cements, abundant white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly detritus, hard, very poor visual porosity, no oil fluorescence. |
|  | 10 | CLAYSTONE: as for 1182-1185m. |
| 1188-1191 | 90 | SANDSTONE: light to medium green grey, very fine to medium, dominantly fine, subangular to subrounded, moderately sorted, moderate silica and calcareous cements, abundant white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly detritus, trace veining infilled by a soft light brown soapy mineral and minor brick red mineral and calcite, hard, very poor visual porosity, no oil fluorescence. |
|  | 10 | CLAYSTONE: as for 1182-1185m. |
| 1191-1194 | 100 | SANDSTONE: light to medium green grey, very fine to medium, dominantly fine, subangular to subrounded, moderately sorted, moderate silica and calcareous cements, abundant white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly detritus, common veining infilled by a soft light brown soapy mineral and minor brick red mineral and calcite, hard, very poor visual porosity, no oil fluorescence. |
| 1194-1197 | 100 | SANDSTONE: light to medium green grey, very fine to medium, dominantly medium, subangular to subrounded, moderately sorted, strong silica and calcareous cements, abundant white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly detritus, abundant veining infilled by a soft light brown soapy mineral and minor brick red mineral and calcite, very hard, no visual porosity, no oil fluorescence. |
| 1197-1200 | 100 | SANDSTONE: light to medium green grey, very fine to medium, dominantly medium, subangular to subrounded, moderately sorted, strong silica and weak calcareous cements, abundant white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly detritus, trace veining infilled by a soft light brown soapy mineral and minor brick red mineral and calcite, very hard, no visual porosity, no oil fluorescence. |
| 1200-1203 | 100 | SANDSTONE: light to medium green grey, very fine to medium, dominantly medium, subangular to subrounded, moderately sorted, strong silica and weak calcareous cements, abundant white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly detritus, common veining infilled by a soft light brown soapy mineral and minor brick red mineral and calcite, very hard, no visual porosity, no oil fluorescence. |
|  | Trace | COAL: black, subvitreous lustre, blocky to subconchoidal fracture, clean to moderately argillaceous, hard, brittle. |
|  | CUT | The coal has no fluorescence but gives a very weak dull pale yellow white crush cut. |
| 1203-1206 | 100 | SANDSTONE: light to medium green grey, very fine to medium, dominantly medium, subangular to subrounded, moderately sorted, strong silica and calcareous cements, abundant white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly detritus, common to abundant veining infilled by a soft light brown soapy mineral and minor brick red mineral and calcite, very hard, no visual porosity, no oil fluorescence. |
|  | Trace | COAL: as for 1200-1203m. |
| 1206-1209 | 90 | SANDSTONE: light to medium green grey, very fine to medium, dominantly medium, subangular to subrounded, moderately sorted, strong silica and calcareous cements, common white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, common black coaly material, common to abundant veining infilled by a soft light brown soapy mineral and common brick red mineral and calcite, very hard, no visual porosity, no oil fluorescence. |
|  | 10 | CLAYSTONE: as for 1182-1185m. |
|  | Trace | COAL: as for 1200-1203m. |
| 1209-1212 | 100 | SANDSTONE: light to medium green grey, very fine to medium, dominantly medium, subangular to subrounded, moderately sorted, strong silica and calcareous cements, common white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, common black coaly material, abundant veining infilled by a soft light brown soapy mineral and common brick red mineral and calcite, very hard, no visual porosity, no oil fluorescence. |
|  | Trace | COAL: as for 1200-1203m. |
| 1212-1215 | 80 | SANDSTONE: as for 1209-1212m. |
|  | 10 | CLAYSTONE: off white to medium grey to medium green grey to medium brown grey, very silty, often very finely arenaceous with altered lithic grains, trace black carbonaceous flecks, common black coal detritus, trace micromica, common slickensided surfaces, moderately hard, subfissile. |
|  | 10 | COAL: black, subvitreous lustre, platy to subconchoidal fracture - slickensided, clean to moderately argillaceous, trace cut as for 1200-1203m, hard, brittle. |
| 1215-1218 | 80 | SANDSTONE: light to medium green grey, very fine to medium, dominantly medium, subangular to subrounded, moderately sorted, strong silica and calcareous cements, common white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, common black coaly material, abundant veining infilled by a soft light brown soapy mineral and common brick red mineral, abundant crystalline calcite, very hard, no visual porosity, no oil fluorescence. |
|  | 20 | CLAYSTONE: as for 1212-1215m. |
|  | Trace | COAL: as for 1212-1215m. |
| 1218-1221 | 90 | SANDSTONE: light to medium green grey, very fine to medium, dominantly medium, subangular to subrounded, moderately sorted, strong silica and calcareous cements, common white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, common black coaly material, abundant veining infilled by a soft light brown soapy mineral and common brick red mineral, common crystalline calcite, abundant slickensiding, very hard, no visual porosity, no oil fluorescence. |
|  | 10 | CLAYSTONE: as for 1212-1215m. |
|  | Trace | COAL: as for 1212-1215m. |
| 1221-1230 | 100 | SANDSTONE: light to medium green grey, very fine to medium, dominantly medium, subangular to subrounded, moderately sorted, strong silica and calcareous cements, common white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, common black coaly material, abundant veining infilled by a soft light brown soapy mineral and trace brick red mineral, common crystalline calcite, no visual porosity, no oil fluorescence. |
| 1230-1233 | 100 | SANDSTONE: light to medium green grey, very fine to rarely coarse, dominantly medium, subangular to subrounded, moderately sorted, strong silica and calcareous cements, common white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly material, abundant veining infilled by a soft light brown soapy mineral and trace brick red mineral, common crystalline calcite, no visual porosity, no oil fluorescence. |
|  | Trace | COAL: as for 1212-1215m. |
| 1233-1239 | 100 | SANDSTONE: light to medium green grey, very fine to coarse, dominantly medium, subangular to subrounded, moderately sorted, strong silica and calcareous cements, common white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly material, abundant veining infilled by a soft light brown soapy mineral and trace brick red mineral, common crystalline calcite, no visual porosity, no oil fluorescence. |
| 1239-1242 | 70 | SANDSTONE: light to medium green grey, very fine to fine, dominantly very fine, subangular to subrounded, moderately sorted, strong silica and calcareous cements, common white argillaceous matrix, abundant altered feldspar and grey green lithic grains, trace orange brown and black lithic grains, trace quartz grains, trace black coaly material, abundant veining infilled by a soft light brown soapy mineral and trace brick red mineral, common crystalline calcite, no visual porosity, no oil fluorescence. |
|  | 30 | CLAYSTONE: off white to medium grey to medium green grey to medium brown grey, very silty, often very finely arenaceous with altered lithic grains, trace black carbonaceous flecks, common black coal detritus, trace micromica, common slickensided surfaces, abundant veining infilled by a soft light brown soapy mineral and trace brick red mineral, common crystalline calcite, moderately hard, subfissile. |
| 1242-1244 | 40 | SANDSTONE: as for 1239-1242m. |
|  | 60 | CLAYSTONE: off white to medium grey to medium green grey to medium brown grey, very silty, often very finely arenaceous with altered lithic grains, trace black carbonaceous flecks, common black coal detritus, trace micromica, common slickensided surfaces, common veining infilled by a soft light brown soapy mineral and trace brick red mineral, common crystalline calcite, moderately hard, subfissile. |